1
 Ordered and Disordered Contributions to Lattice Thermal Conductivity
Jason Larkin and Alan McGaughey
Nanoscale Transport Phenomena Laboratory
Carnegie Mellon Department of Mechanical Engineering
http://ntpl.me.cmu.edu/
07/12/2012

---
Thermal Transport in Disordered Materials
2
Phonon picture valid with perturbations. Perfect systems and dilute alloys
- Phonon picture only valid for very long wavelengths. Alloy and amorphous
- Localized vibrations (diffusons) become important.
(order)
(disorder)

---
Thermal Transport in Disordered Materials: Applications
3
- Crystal → Large Unit Cell → amorphous

---
Theoretical Models
4
Phonons (ordered): Interacting Phonon Gas
phonon-phonon (anharmonicity), defects (dilute), boundaries, (phonon-diffuson?)
Diffusons (disordered): Allen-Feldman Theory
diffuson-diffuson, (boundaries, diffuson-phonon?)
/ V
/ V
LD : Lattice Dynamics => frequencies, group velocities, eigenvectors for phonon mapping, harmonic disordered thermal conductivity
MD: Molecular Dynamics => Green-Kubo, trajectories for phonon mapping, phonon/diffuson lifetimes
Classical Only: for solids, Force Constant MD can
?

---
Modeling Tools
5
	Predicted quantities	Computational cost	Code availability
Green-Kubo (GK) w/ Molecular Dynamics (MD)	Thermal conductivity	Classical	Several
Harmonic Lattice Dynamics (HLD)	Vibrational frequencies, eigenvectors, group velocities, diffuson properties (Allen-Feldman (AF))	Classical/Ab-Initio	Several
Normal Mode Decomposition (NMD) w/ HLD and MD	Thermal conductivity, Vibrational frequencies, lifetimes	Classical	None
LD : Lattice Dynamics => frequencies, group velocities, eigenvectors for phonon mapping, harmonic disordered thermal conductivity
MD: Molecular Dynamics => Green-Kubo, trajectories for phonon mapping, phonon/diffuson lifetimes
Classical Only: for solids, Force Constant MD can

---
Systems Modeled: LJ Alloys and Amorphous
5
Unit cell
Virtual Crystal (VC) approximation
T=10K
c=0.5, mavg = 2.0
System sizes: up to 4000 atoms, 6 nm
Unit cell
LD : Lattice Dynamics => frequencies, group velocities, eigenvectors for phonon mapping, harmonic disordered thermal conductivity
MD: Molecular Dynamics => Green-Kubo, trajectories for phonon mapping, phonon/diffuson lifetimes
Classical Only: for solids, Force Constant MD can
= 0

---
Thermal Conductivity: System-Level
6
Green-Kubo
Heat current J has all effects of MD (anharmonicity, defects, etc.)
Heat current J has KE and PE parts.
J is difficult to define using ab-initio calculations.
T=10K

---
Normal Mode Decomposition (NMD)
7
NMD: Time-Domain
NMD: Frequency-Domain
Kinetic Energy

---
Normal Mode Decomposition (NMD)
8
Virtual Crystal
Gamma point
= 0

---
Thermal Conductivity: System- and Carrier-Level
9
Virtual Crystal approximation and phonon scaling relations work well!
Anharmonic Lattice Dynamics + Defect scaling =
PHYSICAL REVIEW B 85, 184303 (2012)
PRL 106, 045901 (2011)

---
Ordered and Disordered Vibrations
10
Ioffe-Regel Limit:
Cahill-Pohl Model:
Solid State Communications 70 (1989) 927-930.
/
s
/

---
Ordered and Disordered Vibrations
11
Phonons
Diffuson
/
>
= sound speed
Phonon:
Diffuson:
PHIL. MAG. B 79, 1715-1731 (1999)
PHIL. MAG. B 79, 1747-1754 (1999)
Dynamic Structure Factor:
Low-frequency modes can identify a wavelength, not possible in general:
?
s
s
<
s
(
)
1/2
s

---
Predicted Thermal Conductivity
12

---
Cumulative Thermal Conductivity
13
- Boundary Scattering:
Cumulative Thermal Conductivity
- Large c alloys and amorphous vibrations have decreased MFP
- Boundary scattering less effective for length scales >10 nm

---
Bulk Thermoelectrics
14
- Bulk thermoelectric systems are “soft” (small group velocities, small lifetimes)
- MFPs are typically < 100 nm, boundary scattering not effective
- Alloying can still be effective
PHYSICAL REVIEW B 85, 184303 (2012)

---
Amorphous Silicon
15
- a-Si thermal conductivity displays clear film thickness dependance
- Indicates a phonon-like boundary scattering dependance
- Ordered/Disordered analysis could measure the MFP spectrum in a-Si
APPLIED PHYSICS LETTERS 98, 144101 ͑2011͒

---
Questions
16

---
Green-Kubo
2
Heat current J has all effects of MD (anharmonicity, defects, etc.)
Heat current J has KE and PE parts.
J is difficult to define using ab-initio calculations.

---
Normal Mode Decomposition (NMD)
34
Perfect system: vibrations are phonons with an allowed wavevector
Perturbed system: vibrations are phonons with an allowed wavevector (dilute alloy).
Virtual Crystal (VC) approximation.
Disordered system: vibrations are phonons/diffusons. Vibrations analyzed at Gamma point.
= 0