## Slide 1: Predicting Phonon Properties of Defected Systems using the Spectral Energy Density Jason Larkin Alan McGaughey http://ntpl.me.cmu.edu/ 5/24/2011

## Slide 2: Dielectric Thermal Conductivity
Dielectric crystal = Electrical Insulator
Ex: Si, Ge
Dielectric Thermal Conductivity:
Phonons are lattice vibrations…

## Slide 3: Phonons
kspring
matom
Lattice vibrations (Phonons) are travelling waves:
Waves that can exist depend on system size.
When system is very large (bulk)…
=
kspring
matom
Phonons Interact:
Non-linear springs cause phonons to interact.

## Slide 4: Thermal Conductivity Phonon Gas
Phonons interact: with each other, defects, boundaries, etc.
If system L >> :
Kinetic Theory Phonon Gas:
Tc
TH
Phonons interact

## Slide 5: Molecular Dynamics and Spectral Energy Density
Molecular Dynamics
- Lennard-Jones:
Spectral Energy Density
Frequency, group velocity and lifetimes of phonons from Molecular Dynamics.

## Slide 6: Spectral Energy Density
- No phonon knowledge required a priori.
Can measure:
mass
velocity
Spatial and temporal fourier txn.
allowed wavevectors and equil. positions
PHYSICAL REVIEW B 81, 081411R 2010

## Slide 7: Spectral Energy Density Pure System
Spectral Energy Density (SED): system energy in frequency and wavevector space.
Broad peak = short lifetime
SED(ω)
ω (rads/ps)
PHYSICAL REVIEW B 81, 081411R 2010

## Slide 8: Spectral Energy Density of Defected System
Defect = Disorder = non-periodic
m1=1.0 m2=3.0
Phonon picture still valid?
m11-xm2x

## Slide 9: Bulk Thermal Conductivity Prediction
Predict thermal conductivity up to x=0.1 (weakly perturbed)
Typically:
m1/m2 = 3 (mSi/mGe≈3)
Chart: T=5K
| 0 | 1.0000000000000011E-2 | 5.0000000000000037E-2 | 0.1
SED | 3.5065 | 1.0393 | 0.38435 | 0.19827
Alloy Limit | 3.3269 | 1.0749 | 0.32 | 0.19 | 0.1122 | 0.1
PRL 106, 045901 (2011)

## Slide 10: Thermal Conductivity of Thin Films
Increasing
Disorder
τ(ω) (ps)
ω (rads/ps)
198 – 3 nm
29 – 0.65 nm
Pure
Defected
Chart: T=5K
| 0 | 1.0000000000000005E-2 | 0.05 | 0.1
SED | 3.5065 | 1.0393 | 0.38435 | 0.19827
Alloy Limit | 3.3269 | 1.0749 | 0.32 | 0.19 | 0.1122 | 0.1

## Slide 11: Thermal Conductivity Amorphous (Heavily Disordered) Materials

## Slide 12: Discussion
Dielectric thermal conductivity can be described by Kinetic Theory (bulk system).
Molecular Dynamics and Spectral Energy Density can measure phonon properties.
Phonon properties can be predicted for “weakly” perturbed systems, analyzed on mode by mode basis.
Chart: 
| 0 | 0.25 | 0.5 | 0.75000000000000111 | 1 | 1.25 | 1.5 | 1.75 | 2 | 2.25 | 2.5 | 2.75 | 3 | 3.25 | 3.5 | 3.75 | 4 | 4.25 | 4.5 | 4.75 | 5 | 5.25 | 5.5 | 5.75 | 6 | 6.25 | 6.5 | 6.75 | 7 | 7.25 | 7.5 | 7.75 | 8 | 8.25 | 8.5 | 8.75 | 9 | 9.25 | 9.5 | 9.75 | 10 | 10.25 | 10.5 | 10.75 | 11 | 11.25 | 11.5 | 11.75 | 12
 | 0.0043905 | 0.0047776 | 0.0052182 | 0.0057224 | 0.0063032 | 0.0069767 | 0.0077637 | 0.0086911 | 0.0097942 | 0.01112 | 0.012732 | 0.01472 | 0.017206 | 0.020372 | 0.024485 | 0.029959 | 0.037448 | 0.048047 | 0.063662 | 0.08781 | 0.12732 | 0.19588 | 0.31831 | 0.5093 | 0.63662 | 0.5093 | 0.31831 | 0.19588 | 0.12732 | 0.08781 | 0.063662 | 0.048047 | 0.037448 | 0.029959 | 0.024485 | 0.020372 | 0.017206 | 0.01472 | 0.012732 | 0.01112 | 0.0097942 | 0.0086911 | 0.0077637 | 0.0069767 | 0.0063032 | 0.0057224 | 0.0052182 | 0.0047776 | 0.0043905
SED(ω)

## Slide 13: Questions

## Slide 14: Phonon Gas
Chart: 
| 0 | 6.2831853071795868E-2 | 0.12566370614359168 | 0.18849555921538771 | 0.25132741228718347 | 0.31415926535898003 | 0.37699111843077515 | 0.4398229715025726 | 0.50265482457436683 | 0.56548667764616267 | 0.62831853071795718 | 0.69115038378975358 | 0.75398223686155064 | 0.81681408993334559 | 0.87964594300514398 | 0.94247779607693749 | 1.0053096491487337 | 1.0681415022205301 | 1.1309733552923256 | 1.1938052083641193 | 1.2566370614359181 | 1.3194689145077141 | 1.38230076757951 | 1.4451326206513053 | 1.5079644737230991 | 1.5707963267948972 | 1.6336281798666941 | 1.6964600329384891 | 1.7592918860102829 | 1.822123739082081 | 1.8849555921538781 | 1.9477874452256729 | 2.0106192982974691 | 2.0734511513692637 | 2.1362830044410597 | 2.1991148575128623 | 2.2619467105846542 | 2.3247785636564484 | 2.3876104167282399 | 2.4504422698000377 | 2.5132741228718372 | 2.5761059759436269 | 2.6389378290154282 | 2.7017696820872241 | 2.7646015351590201 | 2.8274333882308182 | 2.8902652413026142 | 2.9530970943744079 | 3.0159289474462039 | 3.0787608005180003 | 3.1415926535897958
 | 0 | 0.062822 | 0.12558 | 0.18822 | 0.25067 | 0.31287 | 0.37476 | 0.43629 | 0.49738 | 0.55798 | 0.61803 | 0.67748 | 0.73625 | 0.7943 | 0.85156 | 0.90798 | 0.96351 | 1.0181 | 1.0717 | 1.1242 | 1.1756 | 1.2258 | 1.2748 | 1.3226 | 1.3691 | 1.4142 | 1.4579 | 1.5002 | 1.541 | 1.5803 | 1.618 | 1.6542 | 1.6887 | 1.7215 | 1.7526 | 1.782 | 1.8097 | 1.8355 | 1.8596 | 1.8818 | 1.9021 | 1.9206 | 1.9372 | 1.9518 | 1.9646 | 1.9754 | 1.9842 | 1.9911 | 1.9961 | 1.999 | 2
 | 0 | 0.062832 | 0.12566 | 0.1885 | 0.25133 | 0.31416 | 0.37699 | 0.43982 | 0.50265 | 0.56549 | 0.62832 | 0.69115 | 0.75398 | 0.81681 | 0.87965 | 0.94248 | 1.0053 | 1.0681 | 1.131 | 1.1938 | 1.2566 | 1.3195 | 1.3823 | 1.4451 | 1.508 | 1.5708 | 1.6336 | 1.6965 | 1.7593 | 1.8221 | 1.885 | 1.9478 | 2.0106 | 2.0735 | 2.1363 | 2.1991 | 2.2619 | 2.3248 | 2.3876 | 2.4504 | 2.5133 | 2.5761 | 2.6389 | 2.7018 | 2.7646 | 2.8274 | 2.8903 | 2.9531 | 3.0159 | 3.0788 | 3.1416
“Acoustic” Modes
Phonons vs. Photons:
matom
Non-linear springs
Phonons interact with each other
Interacting Gas…
Chart: 
Phonon Spectral Distribution

## Slide 15: Dispersion of Disordered System
Quasi-Harmonic Lattice Dyanmics:
matom
a=f(T)
Chart: K[x 0 0]
| 0.5 | 0.37500000000000028 | 0.25 | 0.125
x=0.1 SED | 4.9593 | 3.8962 | 2.6346 | 1.3574
 | 6.8886 | 5.3452 | 3.5972 | 1.7956
x=0 QHLD | 6.0799 | 5.4554 | 4.7789 | 4.0564 | 3.2943 | 2.4999 | 1.6806 | 0.8445 | 0
 | 8.5339 | 7.5847 | 6.5798 | 5.5323 | 4.4539 | 3.3547 | 2.2424 | 1.1228 | 0
m=1.2 QHLD | 0 | 0.76598 | 1.524 | 2.2664 | 2.9855 | 3.6744 | 4.3264 | 4.9355 | 5.4962
QHLD | 0 | 1.0136 | 2.0245 | 3.029 | 4.0219 | 4.9958 | 5.9413 | 6.839 | 7.692
T=5K
x=0.1
mx=0.1
Virtual Crystal Approximation:
mx=0.1 = (0.9m1+0.1m2) = 1.2