## Slide 1: Thermal Conductivity Predictions for Nanostructures by Phonon Free Path Sampling
Ankit Jain
Advisor: Alan McGaughey

## Slide 2: Motivation
Nanostructures are important part of our life.
They are present in semiconductor laser, solar energy conversion, thermoelectric energy conversion devices, nano-sensors, etc.
Thermal properties of nanostructures are considerably different from bulk materials.
Can be advantageous in some applications like thermoelectric energy conversion while disadvantageous in other applications like solar cells.

## Slide 3: Outline
Introduction
Phonon Scattering Mechanisms
Results
Conclusions

## Slide 4: Introduction
Heat Carriers: PHONONS, electrons.
Thermal Conductivity: Boltzmann Transport Equation,
Specific heat per phonon mode
Phonon mode group velocity
Relaxation time
Phonons specific heat:
Bose-Einstein Statistics
Group velocity:
Group Velocity is the slope of phonon dispersion curve
Time taken (distance travelled) by phonons before getting scattered.
Need to know different phonon scattering mechanisms in material.
  Turney et al., PRB 79, 064301 (2009)

## Slide 5: Phonon Scattering Mechanisms
Phonon-phonon scattering:
  All Temperatures.
  All length scales.
  Anharmonic lattice dynamics calculations.
Phonon-boundary scattering:
  All Temperatures.
  Length scales compared to phonon-phonon mean free path.
  Approaches like Matthiessean rule, Casimir limit, etc.
Other scattering mechanisms:
  Electrons, dislocations, isotopes, etc.
  Negligible as compared to other two scattering mechanisms at room temperature and for perfect crystals.
Notes: Important in Zoey’s case

## Slide 6: Phonon-Boundary Scattering: Matthiessean Rule
Different Scattering Mechanisms are independent of each other.
Total Scattering Rate
Phonon-phonon scattering rate
Phonon-boundary scattering rate
Other phonon scattering rates
=
+
+
Assumes single length scale for phonon-phonon and phonon-boundary scattering.
Complex Geometries:

## Slide 7: Sampling: An Alternative Approach for Phonon-Boundary Scattering
Random sampling of phonons initial position inside the material
Sampled from Poisson distribution
1000 samples for each phonon mode
  McGaughey et al., APL 100, 061911 (2012)

## Slide 8: Bulk Thermal Conductivity
Bulk phonon properties from Esfarjani, MIT.
Bulk properties are calculated using ab-initio technique without using any potential.
32000 phonon modes are used for capturing first Brillioun zone.
All thermal conductivity calculation are done at 300K in this work.
Bulk thermal conductivity:
Simulation: 132 W/mK.
Experiments: 143 W/mK.
  Esfarjani et al., PRB 84, 085204 (2011)

## Slide 9: Results: Thin Films

## Slide 10: Porous Thin Films
a: Pore separation
t: Film thickness
d: Pore diameter
Thin film with an array of cylindrical thorough holes

## Slide 11: Results: Porous Thin Films
Film thickness = 500 nm

## Slide 12: Results: Porous Thin Films (Contd..)
In-plane thermal conductivity variation with film thickness

## Slide 13: Results: Porous Thin Films (Contd..)
Cross-plane thermal conductivity comparison with experiments
Film thickness = 500 nm
  Hopkins et al.,Nano Letters 11(1), pp 107 (2011)

## Slide 14: Conclusions and Future Work
Sampling approach can be applied for any geometry.
Poisson distribution is assumed as phonon-phonon free path distribution.
In-plane thermal conductivity predictions matches very well with the available experimental data for thin films and porous media.
Cross-plane thermal conductivity predictions are very different from experiments. Presence of oxide layer or some different physics is expected for this discrepancy.

## Slide 15: Thank You