## Slide 1: Predicting Phonon Properties of Defected Systems using the Spectral Energy Density Comparison and Evaluation of Spectral Energy Methods for Predicting Phonon Properties Jason Larkin Alan McGaughey Nanoscale Transport Phenomena Laboratory Carnegie Mellon Department of Mechanical Engineering http://ntpl.me.cmu.edu/ 11/28/2011
1

## Slide 2: Phonon Properties
Thermal Conductivity:
Matthiesen Rule1,2:
1A. J. H. McGaughey et al., Applied Physics Letters 99, 131904 (2011).
2D. P. Sellan, et al., Journal of Applied Physics 108, 113524 (2010).
Nano Letters 9 2009 864-869
Nano Letters 11, 107-112 (2011).
2
Accurate phonon lifetimes are important!

## Slide 3: Phonon Normal Mode Coordinate1,2
Phonon occupation:
Phonon occupation:
3
2D. C. Wallace, Thermodynamics of Crystals.
1M. T. Dove, Introduction to Lattice Dynamics.
Need:
Allowed wavevectors (from crystal):
Atomic velocities (from molecular dynamics):
Eigenvector (from lattice dynamics):
Lattice dynamics requires periodic system.

## Slide 4: Phonon Lifetime from Spectral Energy
Broad peak = short lifetime
Chart: 
| 0 | 0.25 | 0.5 | 0.75000000000000022 | 1 | 1.25 | 1.5 | 1.7500000000000004 | 2 | 2.25 | 2.5 | 2.75 | 3 | 3.25 | 3.5 | 3.75 | 4 | 4.25 | 4.5 | 4.75 | 5 | 5.25 | 5.5 | 5.75 | 6 | 6.25 | 6.5 | 6.75 | 7 | 7.25 | 7.5 | 7.75 | 8 | 8.25 | 8.5 | 8.75 | 9 | 9.25 | 9.5 | 9.75 | 10 | 10.25 | 10.5 | 10.75 | 11 | 11.25 | 11.5 | 11.75 | 12
 | 0.0043905 | 0.0047776 | 0.0052182 | 0.0057224 | 0.0063032 | 0.0069767 | 0.0077637 | 0.0086911 | 0.0097942 | 0.01112 | 0.012732 | 0.01472 | 0.017206 | 0.020372 | 0.024485 | 0.029959 | 0.037448 | 0.048047 | 0.063662 | 0.08781 | 0.12732 | 0.19588 | 0.31831 | 0.5093 | 0.63662 | 0.5093 | 0.31831 | 0.19588 | 0.12732 | 0.08781 | 0.063662 | 0.048047 | 0.037448 | 0.029959 | 0.024485 | 0.020372 | 0.017206 | 0.01472 | 0.012732 | 0.01112 | 0.0097942 | 0.0086911 | 0.0077637 | 0.0069767 | 0.0063032 | 0.0057224 | 0.0052182 | 0.0047776 | 0.0043905
SED(ν)
ω
4

## Slide 5: Proposed Phonon Spectral Energy1,2
Does NOT represent phonon spectral energy!
5
2J. A. Thomas, et al., Physical Review B 81, 081411(R) (2010).
1S. Maruyama, Microscale Thermophysical Engineering 7, 41 (2003).
Need:
Allowed wavevectors:
Atomic velocities:
Eigenvector from lattice dynamics:
Measure lifetimes in defected/disordered systems!

## Slide 6: Proposed Phonon Spectral Energy
6
2J. A. Thomas, et al., Physical Review B 81, 081411(R) (2010).
1S. Maruyama, Microscale Thermophysical Engineering 7, 41 (2003).
- Originally proposed to measure dispersion in CNT.
- Measured lifetime reduction in water-filled CNT and on SiO2.
6J. Shiomi, et al., Physical Review B 84, 104302 (2011).
- Lifetimes in MgO and Half-Heusler alloys from ab-initio
3Z.-Y. Ong, et al., Physical Review B 84, 104302 (2011).
5N. de Koker, Physical Review Letters 103, 125902 (2009).
- Lifetimes in bulk PbTe agree with experiment
4B. Qiu, et al., Computational Materials Science 53, 278285 (2011).

## Slide 7
Clear linewidth variations:
7
LJ Ar K = [π/2a 00]
Area under curve is total phonon kinetic energy only for
Phonon Spectral Energy Comparison
Peak locations (freq) agree well.

## Slide 8: 3 Case Studies
Lennard-Jones Ar: well-studied, computationally cheap
Stillinger-Weber Silicon1: “stiff” system (high frequencies, large group velocities, long lifetimes).
Carbon nanotube using REBO2,3: test/validate previous work.
2D. W. Brenner, et al., Journal of Physics: Condensed Matter 14, 783 (2002).
1F. H. Stillinger and T. A. Weber, Physical Review B 31, 5262 (1985).
3J. A. Thomas, et al., Physical Review B 81, 081411(R) (2010).
8

## Slide 9: Case Study: LJ Lifetimes
Frequencies agree well, increasing scatter with T(K)
Lifetimes large scatter independent of T(K)
9

## Slide 10: Thermal Conductivity Predictions: LJ
10
1J. E. Turney, et al., Physical Review B 79, 064301 (2009).
2J. A. Thomas, et al., Physical Review B 81, 081411(R) (2010).
LJ results for and other methods agree1, does not.
Results from exact same molecular dynamics data.

## Slide 11: Case Study: SW Si and CNT Lifetimes
Frequencies agree well
Lifetimes large scatter
Frequencies agree well
Lifetimes large scatter
11
Si
CNT

## Slide 12: Thermal Conductivity Predictions: SW Si and CNT
12
1J. E. Turney, et al., Physical Review B 79, 064301 (2009).
2J. A. Thomas, et al., Physical Review B 81, 081411(R) (2010).
- SW Si and CNT2 results indicate no systematic behavior for .

## Slide 13: Proposed Phonon Spectral Energy Density
Should NOT be used to predict lifetimes or thermal conductivity!
Can accurately measure frequencies, even in disordered systems.
13

## Slide 14: Dispersion in Disordered Systems
c=0.5
me=2
LJ alloys with:
ma = 1
mb = 3
- Dispersion well approx. by lattice dynamics w/me
- Original purpose for 1!
1 S. Maruyama, Microscale Thermophysical Engineering 7, 41 (2003).
14
K = [100]

## Slide 15: Questions
Acknowledgments:
This work is supported by AFOSR award FA95501010098.
15

## Slide 16: Defect Scattering
Matthiesen Rule:
Rayleigh scattering:
16

## Slide 17: Thermal Conductivity of Thin Films
Chart: T=5K
| 0 | 1.0000000000000005E-2 | 0.05 | 0.1
SED | 3.5065 | 1.0393 | 0.38435 | 0.19827
Alloy Limit | 3.3269 | 1.0749 | 0.32 | 0.19 | 0.1122 | 0.1
GK
17